Supplementary information

Excitonic coupling of electronic transitions in oligomeric phthalocyanine zinc(II) complexes

Sergey G. Makarov,*a Sergey Yu. Ketkov a and Dieter Wöhrle b

Fig. S1.

Fig. S2.

Table S1.

| Shift, Å |  | Q-band transition energy, eV |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Δz | Δx | BG | AG | BU (X) | AU (Y) |
| 0 | 17.0 | 1.805 | 1.834 | 1.770 | 1.819 |
|  | 18.0 | 1.805 | 1.829 | 1.781 | 1.817 |
|  | 20.0 | 1.806 | 1.823 | 1.792 | 1.815 |
|  | 22.0 | 1.806 | 1.820 | 1.798 | 1.813 |
|  | 24.0 | 1.807 | 1.817 | 1.801 | 1.812 |
| 3.5 | 0.0 | 1.147 | 1.147 | 1.914 | 1.914 |
|  | 1.0 | 1.511 | 1.401 | 1.895 | 1.888 |
|  | 1.75 | 1.550 | 1.595 | 1.841 | 1.875 |
|  | 2.0 | 1.504 | 1.602 | 1.823 | 1.881 |
|  | 2.25 | 1.485 | 1.598 | 1.809 | 1.888 |
|  | 3.0 | 1.588 | 1.613 | 1.800 | 1.881 |
|  | 3.5 | 1.666 | 1.647 | 1.810 | 1.864 |
|  | 4.0 | 1.688 | 1.672 | 1.817 | 1.857 |
|  | 5.0 | 1.711 | 1.719 | 1.803 | 1.860 |
|  | 5.25 | 1.714 | 1.732 | 1.797 | 1.859 |
|  | 6.0 | 1.711 | 1.763 | 1.777 | 1.848 |
|  | 7.0 | 1.742 | 1.800 | 1.768 | 1.834 |
|  | 8.0 | 1.748 | 1.824 | 1.765 | 1.817 |
|  | 10.0 | 1.774 | 1.853 | 1.738 | 1.813 |
|  | 10.5 | 1.778 | 1.851 | 1.743 | 1.814 |
|  | 12.0 | 1.786 | 1.850 | 1.752 | 1.814 |
|  | 14.0 | 1.797 | 1.842 | 1.763 | 1.818 |
|  | 16.0 | 1.802 | 1.833 | 1.778 | 1.817 |
|  | 18.0 | 1.804 | 1.826 | 1.789 | 1.815 |
|  | 20.0 | 1.805 | 1.822 | 1.795 | 1.814 |
| 4.0 | 0.0 | 1.520 | 1.520 | 1.900 | 1.900 |
|  | 2.0 | 1.635 | 1.651 | 1.866 | 1.886 |
|  | 4.0 | 1.702 | 1.705 | 1.835 | 1.866 |
|  | 5.0 | 1.726 | 1.737 | 1.818 | 1.858 |
|  | 6.0 | 1.739 | 1.770 | 1.800 | 1.846 |
|  | 8.0 | 1.762 | 1.821 | 1.778 | 1.825 |
|  | 10.0 | 1.777 | 1.845 | 1.762 | 1.816 |
|  | 12.0 | 1.788 | 1.845 | 1.764 | 1.816 |
|  | 14.0 | 1.797 | 1.839 | 1.771 | 1.817 |
|  | 16.0 | 1.802 | 1.831 | 1.782 | 1.816 |
|  | 18.0 | 1.804 | 1.825 | 1.790 | 1.815 |
|  | 20.0 | 1.805 | 1.821 | 1.796 | 1.814 |
| 5.0 | 0.0 | 1.691 | 1.691 | 1.881 | 1.881 |
|  | 2.0 | 1.707 | 1.708 | 1.868 | 1.874 |
|  | 2.5 | 1.713 | 1.714 | 1.862 | 1.872 |
|  | 4.0 | 1.734 | 1.740 | 1.843 | 1.861 |
|  | 5.0 | 1.747 | 1.761 | 1.829 | 1.852 |
|  | 6.0 | 1.758 | 1.782 | 1.816 | 1.844 |
|  | 7.0 | 1.766 | 1.801 | 1.805 | 1.836 |
|  | 7.5 | 1.770 | 1.809 | 1.800 | 1.832 |
|  | 8.0 | 1.773 | 1.816 | 1.796 | 1.829 |
|  | 10.0 | 1.783 | 1.834 | 1.784 | 1.820 |
|  | 12.0 | 1.791 | 1.837 | 1.780 | 1.817 |
|  | 14.0 | 1.797 | 1.833 | 1.782 | 1.816 |
|  | 15.0 | 1.800 | 1.831 | 1.785 | 1.816 |
|  | 16.0 | 1.802 | 1.828 | 1.788 | 1.816 |
|  | 18.0 | 1.804 | 1.824 | 1.793 | 1.815 |
|  | 20.0 | 1.805 | 1.820 | 1.797 | 1.814 |
| 6.0 | 0.0 | 1.731 | 1.731 | 1.866 | 1.866 |
|  | 2.0 | 1.738 | 1.739 | 1.858 | 1.862 |
|  | 3.0 | 1.745 | 1.749 | 1.850 | 1.858 |
|  | 4.0 | 1.753 | 1.761 | 1.841 | 1.852 |
|  | 6.0 | 1.769 | 1.788 | 1.821 | 1.840 |
|  | 8.0 | 1.779 | 1.812 | 1.805 | 1.829 |
|  | 9.0 | 1.783 | 1.820 | 1.799 | 1.824 |
|  | 10.0 | 1.787 | 1.826 | 1.794 | 1.821 |
|  | 12.0 | 1.793 | 1.830 | 1.790 | 1.818 |
|  | 14.0 | 1.798 | 1.828 | 1.790 | 1.816 |
|  | 16.0 | 1.802 | 1.825 | 1.793 | 1.815 |
|  | 18.0 | 1.804 | 1.822 | 1.796 | 1.814 |
|  | 20.0 | 1.805 | 1.819 | 1.799 | 1.813 |
| 8.0 | 0.0 | 1.767 | 1.767 | 1.845 | 1.845 |

* ΔE (ZnPc) = 1.809 eV (EU)

Table S2.

| Shift, Å |  | Q-band transition energy, eV |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Δz | Δx | BG | AG | BU (X) | AU (Y) |
| 0 | 15.0 | 1.782 | 1.832 | 1.783 | 1.831 |
|  | 16.0 | 1.789 | 1.828 | 1.788 | 1.826 |
|  | 18.0 | 1.797 | 1.823 | 1.795 | 1.820 |
|  | 20.0 | 1.802 | 1.819 | 1.799 | 1.817 |
| 3.5 | 0.0 | 1.147 | 1.147 | 1.914 | 1.914 |
|  | 1.75 | 1.586 | 1.614 | 1.875 | 1.886 |
|  | 2.0 | 1.555 | 1.611 | 1.869 | 1.883 |
|  | 3.5 | 1.617 | 1.689 | 1.812 | 1.893 |
|  | 4.0 | 1.609 | 1.715 | 1.791 | 1.895 |
|  | 5.25 | 1.650 | 1.773 | 1.778 | 1.866 |
|  | 6.0 | 1.634 | 1.799 | 1.720 | 1.869 |
|  | 7.0 | 1.638 | 1.832 | 1.723 | 1.870 |
|  | 8.0 | 1.697 | 1.833 | 1.750 | 1.862 |
|  | 10.0 | 1.736 | 1.839 | 1.759 | 1.852 |
|  | 10.5 | 1.742 | 1.837 | 1.761 | 1.850 |
|  | 12.0 | 1.763 | 1.835 | 1.772 | 1.841 |
|  | 14.0 | 1.782 | 1.830 | 1.784 | 1.831 |
|  | 16.0 | 1.793 | 1.825 | 1.792 | 1.824 |
|  | 18.0 | 1.799 | 1.821 | 1.797 | 1.819 |
| 4.0 | 0.0 | 1.520 | 1.520 | 1.900 | 1.900 |
|  | 2.0 | 1.636 | 1.663 | 1.871 | 1.891 |
|  | 4.0 | 1.663 | 1.734 | 1.819 | 1.888 |
|  | 6.0 | 1.688 | 1.799 | 1.776 | 1.872 |
|  | 8.0 | 1.719 | 1.830 | 1.769 | 1.859 |
|  | 10.0 | 1.747 | 1.836 | 1.769 | 1.849 |
|  | 12.0 | 1.769 | 1.833 | 1.777 | 1.839 |
|  | 14.0 | 1.785 | 1.828 | 1.787 | 1.830 |
|  | 16.0 | 1.794 | 1.824 | 1.793 | 1.823 |
|  | 18.0 | 1.799 | 1.821 | 1.797 | 1.819 |
| 5.0 | 0.0 | 1.691 | 1.691 | 1.881 | 1.881 |
|  | 2.0 | 1.701 | 1.714 | 1.865 | 1.878 |
|  | 2.5 | 1.704 | 1.723 | 1.857 | 1.878 |
|  | 4.0 | 1.714 | 1.757 | 1.833 | 1.873 |
|  | 5.0 | 1.722 | 1.780 | 1.817 | 1.868 |
|  | 6.0 | 1.730 | 1.799 | 1.804 | 1.863 |
|  | 7.5 | 1.742 | 1.818 | 1.790 | 1.854 |
|  | 8.0 | 1.746 | 1.822 | 1.788 | 1.852 |
|  | 10.0 | 1.763 | 1.829 | 1.783 | 1.843 |
|  | 12.0 | 1.778 | 1.828 | 1.785 | 1.834 |
|  | 14.0 | 1.789 | 1.826 | 1.791 | 1.827 |
|  | 15.0 | 1.792 | 1.824 | 1.793 | 1.824 |
|  | 16.0 | 1.796 | 1.822 | 1.795 | 1.822 |
|  | 18.0 | 1.800 | 1.820 | 1.798 | 1.818 |
| 6.0 | 0.0 | 1.731 | 1.731 | 1.866 | 1.866 |
|  | 2.0 | 1.735 | 1.743 | 1.856 | 1.865 |
|  | 3.0 | 1.738 | 1.755 | 1.846 | 1.863 |
|  | 4.0 | 1.743 | 1.770 | 1.834 | 1.860 |
|  | 6.0 | 1.752 | 1.798 | 1.812 | 1.853 |
|  | 8.0 | 1.763 | 1.816 | 1.798 | 1.845 |
|  | 9.0 | 1.768 | 1.821 | 1.794 | 1.841 |
|  | 10.0 | 1.774 | 1.823 | 1.792 | 1.837 |
|  | 12.0 | 1.784 | 1.824 | 1.792 | 1.831 |
|  | 14.0 | 1.792 | 1.823 | 1.794 | 1.825 |
|  | 16.0 | 1.797 | 1.821 | 1.797 | 1.821 |
|  | 18.0 | 1.801 | 1.819 | 1.800 | 1.818 |

* ΔE (ZnPc) = 1.809 eV (EU)

Table S3. Main contributions of elementary MO-MO transitions to the Q-band transitions of face-to-face ZnPc dimers

| Δz, Å | Transition |  | Occupied MO |  | Virtual MO |  | Contribution |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Symmetry | Energy, eV | Symmetry | Energy, eV | Symmetry | Energy, eV |  |
| 3.5 | EG | 1.147 | a2g | -6.813 | eg | -1.196 | 5.2% |
|  |  |  | a1u | -6.066 | eu | -1.867 | 93.6% |
|  | EU | 1.914 | a2g | -6.813 | eu | -1.867 | 39.9% |
|  |  |  | a1u | -6.066 | eg | -1.196 | 51.3% |
| 4.0 | EG | 1.520 | a2g | -6.617 | eg | -1.383 | 18.5% |
|  |  |  | a1u | -6.275 | eu | -1.700 | 78.5% |
|  | EU | 1.900 | a2g | -6.617 | eu | -1.700 | 44.7% |
|  |  |  | a1u | -6.275 | eg | -1.383 | 46.8% |
| 5.0 | EG | 1.691 | a2g | -6.503 | eg | -1.530 | 41.7% |
|  |  |  | a1u | -6.434 | eu | -1.596 | 53.6% |
|  | EU | 1.881 | a2g | -6.503 | eu | -1.596 | 45.9% |
|  |  |  | a1u | -6.434 | eg | -1.530 | 46.0% |
| 6.0 | EG | 1.731 | a2g | -6.495 | eg | -1.574 | 46.3% |
|  |  |  | a1u | -6.482 | eu | -1.588 | 48.3% |
|  | EU | 1.866 | a2g | -6.495 | eu | -1.588 | 46.1% |
|  |  |  | a1u | -6.482 | eg | -1.574 | 46.1% |

Fig. S3. Distance dependence of HOMO and LUMO splitting for face-to-face ZnPc dimers (Δx = 0)

Fig. S4. Size dependence of main TD-DFT Q-band transition energies of slipped-stacked ZnPc oligomers (resembling β-ZnPc stacks)

Table S4.

| Shifts, Å | Number of monomers | Q-band transition energies, eV, and oscillator strengths |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Along Zn – meso-N (Fig. 4B) |  | f (AUX) | E [AU (X)] | E [AU (Y)] | f (AUY) |
| Δx = 3.632 Δy = 0.185 Δz = 3.214 (β-ZnPc stack) | 1 | 0.483 | 1.809 | 1.809 | 0.483 |
|  | 2 | 0.715 | 1.766 | 1.887 | 0.696 |
|  | 3 | 0.999 | 1.750 | 1.921 | 0.871 |
|  | 4 | 1.291 | 1.740 | 1.939 | 1.033 |
|  | 5 | 1.521 | 1.735 | 1.951 | 1.188 |
|  | ∞ | 1.518 | 1.724 | 1.970 | 1 (ratio) |
| Along Zn – N bond (Fig. 4A) |  | f (BU) | ΔE [BU (X)] | ΔE [AU (Y)] | f (AU) |
| Δx = 1.75 Δy = 0 Δz = 3.3 (approx. α-ZnPc stack) | 1 | 0.483 | 1.809 | 1.809 | 0.483 |
|  | 2 | 0.568 | 1.801 | 1.852 | 0.604 |
|  | 3 | 0.683 | 1.807 | 1.873 | 0.717 |
|  | 4 | 0.798 | 1.810 | 1.884 | 0.825 |
|  | ∞ | 1 (ratio) | 1.807 | 1.900 | 1.074 |
| Δx = 2.0 Δy = 0 Δz = 3.3 (approx. α-ZnPc stack) | 1 | 0.483 | 1.809 | 1.809 | 0.483 |
|  | 2 | 0.562 | 1.772 | 1.868 | 0.631 |
|  | 3 | 0.679 | 1.767 | 1.893 | 0.762 |
|  | 4 | 0.804 | 1.764 | 1.907 | 0.884 |
|  | ∞ | 1 (ratio) | 1.750 | 1.929 | 1.233 |
| Δx = 1.75 Δy = 0 Δz = 3.4 (approx. α-ZnPc stack) | 1 | 0.483 | 1.809 | 1.809 | 0.483 |
|  | 2 | 0.607 | 1.824 | 1.866 | 0.633 |
|  | 3 | 0.737 | 1.835 | 1.891 | 0.760 |
|  | 4 | 0.867 | 1.842 | 1.905 | 0.882 |
|  | ∞ | 1 (ratio) | 1.847 | 1.926 | 1.034 |
| Δx = 2.0 Δy = 0 Δz = 3.4 (approx. α-ZnPc stack) | 1 | 0.483 | 1.809 | 1.809 | 0.483 |
|  | 2 | 0.602 | 1.801 | 1.876 | 0.652 |
|  | 3 | 0.736 | 1.803 | 1.904 | 0.795 |
|  | 4 | 0.877 | 1.804 | 1.920 | 0.933 |
|  | ∞ | 1 (ratio) | 1.800 | 1.945 | 1.133 |

XYZ geometries optimized at B3PW91/6-31G(d) level of DFT