Excitonic coupling of electronic transitions in oligomeric phthalocyanine zinc(II) complexes

Sergei G. Makarov*a, Sergey Yu. Ketkova and Dieter Wöhrleb

aG.A. Razuvaev Institute of Organometallic Chemistry of RAS, Tropinin str. 49, 603950 Nizhniy Novgorod, Russia

bUniversität Bremen, Institut für Angewandte und Physikalische Chemie, P.O. Box 330440, 28334 Bremen, Germany

Received

Accepted

ABSTRACT:

KEYWORDS: phthalocyanines, oligophthalocyanines, electronic transitions, excitonic coupling, time-dependent DFT

*Correspondence to: Sergei G. Makarov, email: makar@iomc.ras.ru

Introduction

Phthalocyanines (Pc) have found many “real” applications as colorants and materials for electronic devices [1-3]. Successful practical use of phthalocyanines (Pcs) in many fields became possible due to their unique molecular structural diversity, photophysical properties and different arrangements in the solid state. Recent potential applications include organic thin-film transistors [4, 5], near-infrared fluorescent diagnostics and photodynamic immunotherapy of tumors [6].

Photophysical properties of phthalocyanine metal complexes can be modified with peripheral substituents, central metal ion or by extension of the π-system [7-9]. The extended π-system of conjugated Pc oligomers results in large redshifts of the lowest-energy absorption (Q-band). Noncovalent interactions (excitonic coupling) of the Pc π-systems are also known to significantly influence photophysical properties of phthalocyanines in aggregates, non-conjugated dimers and crystals [10-34].

Non-conjugated oligo- and polymeric phthalocyanine assemblies include well-known π-π stacked aggregates in solution [13] and in solid state [2, 3, 14-15]. Besides, non-conjugated oligomers via ligand [10, 23-30, 34], metal–ligand [12, 14, 17, 18, 25], hydrogen-bonded [19] and donor-acceptor systems [20] have also been reported. Two types of arrangement of chromophore molecules in aggregates are usually discussed: with face-to-face configurations, often referred to as H-type aggregates, and edge-to-edge or slipped-stacked configurations, known as J-type aggregates (Fig. 1) [13]. A close proximity of the chromophores causes excitonic coupling of their electronic transitions, which significantly influences their photophysical properties [11, 21-22].

According to Kasha’s theory [22], “face-to-face” molecular dimers (H-aggregates) exhibit a blue-shifted absorption maximum and a suppressed radiative decay rate while “edge-to-edge” and “slipped-stacked” dimers (J-aggregates) exhibit a red-shifted absorption maximum and enhanced radiative decay rate. For dimers with parallel arrangement of chromophores, the interaction of the transition dipoles can be approximated by a simple point-dipole model:

∆E≈μ2(1-3cos2θ)4πεr3	(1)

where μ and r represent the magnitude of the transition moment in the monomer and the center-to-center distance between the molecules, respectively, θ is the angle between the polarization axis and the line between the dipole centers. The energy change ΔE becomes zero at θ = 54.7°, i.e. two molecules behave as an H-aggregate above θ = 54.7° and as a J-aggregate below this angle.

Fig. 1. Excitonic coupling of electronic transitions in molecular dimers

Although many examples of "face-to-face" phthalocyanine dimers, oligomers and aggregates [10, 23-27, 33-34] and a few "edge-to-edge" and "slipped-stack" dimers and aggregates were described [12, 17, 28-31], the exact alignment of the Pc subunits in these systems is not known, except for the crystals where slipped-stacked arrangement is typical for M(II)Pcs [1, 2, 15, 16]. Only a few binuclear Pcs with a linker rigid enough to ensure a well-defined geometry, are known experimentally (Chart 1): a “gable” 1 [32], a “planar” 2 [30], and a “cyclophane” 3 [31] bridged binuclear phthalocyanines with the “edge-to-edge” and “slipped-stack” arrangement (J-dimers). For the “face-to-face” binuclear Pcs (H-dimers) with rigid linkers such as 4 [26] and 5 [27], different conformations are still possible with significantly different excitonic coupling (see below). One example of a supramolecular dimer 6 [12] can be considered rigid although two configurations (“parallel” and “oblique”) are possible.

Fig. 2. Electronic spectra and crystal packing of α- and β-modifications of ZnPc [1]

The effect of aggregation on the Q-band in solution is stronger than solvent effects and typically results in a blue shift from 660-700 nm to 600-640 nm and broadening of the Q-band (H-aggregates) [13]. Similar blue shifts were observed for various covalent and supramolecular cofacial dimers [10, 12, 24-27, 33-34]. In solid state, β-modification of planar M(II)Pcs typically shows a close contact of central metal ion to a meso-N atom of an adjacent molecule in the stack, and an inclination angle of the macrocycles within the stack of ~ 45°. The inclination angle in the α-modification is ~ 30°, and the metal shows a close contact to a pyrrole-N atom of an adjacent molecule. Different arrangements of chromophores result in a significantly different excitonic coupling, leading to a high variability of absorption wavelengths exhibited by crystalline phthalocyanines. Thus, α-modifications of CuPc and ZnPc absorb at λ ~ 625 and ~ 700 nm, β -modifications at λ ~ 650 and ~750 nm, and ε-CuPc at even longer wavelength λ < 820 nm [1-3]. The non-planar Ti(O)Pc with the slipped-stacked arrangement similar to J-aggregates shows a strongly red-shifted Q-band absorption at λ ~ 700 - 900 nm, and an efficient photoinduced charge carrier generation [32].

Slipped-stacked Pc oligomers resemble structural patterns of photosynthetic light-harvesting antenna consisting of bacteriochlorophyll dimers [35], and they are photoactive in contrast to face-to-face Pc oligomers [11, 12, 36] for which a non-radiative decay of the excited states is typical. Therefore, edge-to-edge dimers and J-aggregates are highly desirable to tailor the photophysical properties of Pcs. Cyclophane-fused dimer 3 is fluorescent (Φf = 0.12), a metal-free “gable” dimer 1 is also fluorescent (Φf = 0.55), a “planar” dimer 2 shows a singlet oxygen quantum yield of ΦΔ = 0.08; imidazole-bridged supramolecular dimer 6 is also fluorescent (Φf = 0.26). Surprisingly, for edge-to edge Pc dimer 2 no redshift expected according to Kasha’s theory and the eq. (1) was observed in contrast to slipped-stack 3 showing a strong bathochromic Q-band shift (Table 1) and H-dimers showing a significant hypsochromic shift. It was concluded [8, 31] that π-MO overlap is essential for the efficient excitonic coupling in the Pc dimers, crystals and aggregates, and purely Coulomb coupling of the transition dipoles (eq. (1)) is not enough to explain the observed Q-band shifts. Short-range excitonic coupling in phthalocyanine dimers [36-38] and crystals [36-39] were studied previously by DFT and semi-empirical methods. It was shown that short-range coupling is very sensitive to MO overlap, and is related to electron- and hole-transfer integrals [40]. However, a more systematic study including various arrangements (r and θ) are required to provide a general explanation of the observed excitonic coupling effects in phthalocyanine oligomers and crystals.

To organize chromophores into tailored structures, it is important to predict their photophysical properties. Nowadays, machine-learning methods are growing up for predicting crystal structures of molecular materials [41], which require accurate theoretical description of intermolecular properties. Previously, we have studied UV/Vis/NIR spectra and energy gaps of conjugated oligomeric phthalocyanine zinc (II) complexes by TD-DFT and have shown that calculations with range-separated hybrid functional LC-BLYP provide a good agreement with the experimental spectra [42, 43]. The extrapolated TD-DFT Q-band energy of oligoPcs was compared to a directly calculated band gap of 1D-polyPc.

Here, we benchmark the above-mentioned LC-TDDFT approach on excitonically coupled Q-band transitions in non-conjugated binuclear ZnPcs. Then we use the same method to investigate the influence of the relative position of ZnPc molecules (r and θ in the eq. (1)) on the Q-band transition energies, and finally to explain excitonic coupling effects observed for phthalocyanine aggregates, dimers and crystals.

Results and discussion

Bridged oligophthalocyanines. “Rigid” binuclear Pcs 1 – 3 and 6 were selected to exclude influence of noncovalent interactions (poorly described by DFT [44]) on the relative position of the Pc chromophores.

| 1 (1a with substituents) | 2 (2a with substituents) |
| --- | --- |
| 3 (3a with substituents) | 4a |
| 5a (substituents omitted) | 6 (6a with substituents) |

Chart 1. "Rigid" ZnPc dimers

The calculated Q-band wavelengths and energies for the dimers 1 – 3, 6 without peripheral substituents are compared to experimental wavelengths of their Q-band maxima. The results are listed in the Table 1.

Table 1. Experimental and calculated Q-band wavelengths, energies and intensities for rigid non-conjugated oligoPcs 1 – 3, 6 and their substituted analogues 1a – 3a, 6a

| Cpd. # | Experimental (1a – 3a, 6a) |  | Theoretical (1 – 3, 6) |  |
| --- | --- | --- | --- | --- |
|  | λ, nm (ΔE, eV) | 10-5 ε, M-1·cm-1 | λ, nm (ΔE, eV) | Oscillator strength |
| ZnPc | 674 (1.840) | 3.4 | 685 (1.809) | 0.484 × 2 |
| 1, 1a | 694 (1.787) | 2.9 | 713 (1.738) | 1.050 |
|  | 677 (1.832) | 3.1 | 680 (1.823) | 0.906 |
| 2, 2a | 682 (1.818) | 6.9 | 705 (1.758) | 1.334 |
|  |  |  | 692 (1.790) | 0.912 |
| 3, 3a | 753 (1.647) | 0.84 | 743 (1.667) | 1.276 |
|  | 690 (1.797) | 0.72 | 688 (1.800) | 0.833 |
| 6, 6a | 700 (1.771) | 1.7 | 723 (1.714) | 1.070 |
| (parallel) | 670 (1.851) | 1.2 | 676 (1.832) | 0.749 |

As it is seen from the Table 1, theoretical wavelengths are well in agreement with the experimental ones. Therefore, TD-DFT with a range-separated hybrid functional LC-BLYP correctly predicts the through-space excitonic coupling of the excited states of ZnPcs. For edge-to-edge arrangements in 1 and 2, the redshift expected from eq. (1) is negligible, in contrast to a well-known blue shift for face-to-face arrangements in H-dimers and aggregates [10-12, 24-27, 33-34]. In contrast, for the cyclophane-type dimer 3, significant red shift and splitting of the Q-band is revealed both theoretically and experimentally. The nearly zero red shift predicted by Kasha’s theory for edge-to-edge dimers 1 and 2 was explained previously [8, 29] by the absence of the π-π overlap and by the intermolecular π-electron delocalization. Thus, it is important to study whether a general Coulomb dipole-dipole model (eq. (1)) is applicable for oligoPcs, or the observed excitonic coupling in phthalocyanine aggregates, dimers and crystals is a system-specific short-range effect determined by the π-π overlap.

Excitonic coupling between phthalocyanine molecules. To evaluate excitonic coupling effects in oligoPcs, model zinc phthalocyanine dimers with face-to-face, slipped-stacked and edge-to-edge parallel arrangements of the Pc rings with parallel shifts (Δx) from 0 to 20 Å, and interplane distances (Δz) from 0 to 6 Å, were studied by TD-DFT. The corresponding distances (r) and angles (θ) can be easily calculated to compare TD-DFT transition energies to those predicted by the equation (1). Pcs show intense π → π* absorption bands in the visible region. The Q-band corresponds to the doubly degenerate HOMO (a1u) → LUMO (eg) transition (Fig. 3) [45]. For a Pc dimer, there are four Q-band transitions arising from the excitonic splitting of two degenerate EU transitions of a single Pc chromophore: the allowed BU (x-polarized along the shift direction) and AU (y-polarized) excitations (oscillator strengths f ≈ 0.5), and two forbidden transitions, AG and BG (f ≈ 0), corresponding to the opposite orientation of the monomers’ transition dipoles (Fig. 5). MOs of Pc oligomers can be approximately described as linear combinations of the monomers’ MOs [11, 12]. Due to the π-π overlap, the bonding-antibonding interactions between these MOs result in splitting of the corresponding energy levels and, for infinite stacks, to the formation of valence and conduction bands [36, 40]. The dependence of these energies on the arrangement of the Pc molecules (see Fig. 4) is shown in Fig. 6 for the shift along the Zn-N bond (Fig. 4A, which approximately. reproduces the stack arrangement in α-ZnPc). The corresponding transition energies are listed in Table S1. For the shift along meso-N – Zn (Fig. 4B, which approximately. reproduces the stack arrangement in β-ZnPc), the results are shown in Fig. S1 and Table S2.

Fig. 3. Frontier MOs of ZnPc (front and side views)

Fig. 4. Arrangements of the monomers in slipped-stacked ZnPc dimers

Fig. 5. Frontier MO splitting and Q-band transitions in slipped-stacked ZnPc dimers. Point groups?

Fig. 6. TD-DFT Q-band transition energies vs. parallel shifts (Δx) of two Pc molecules (arrangement in Fig. 4A). Forbidden transitions are shown by dashed lines. Units? Black dashed lines?

Angle dependence. For parallel transition dipoles, the dependence of the excitonic splitting on angle θ (Fig. 2) is approximately described by the equation (1). With “face-to-face” arrangement, the allowed X-oriented BU transition is blue-shifted, whereas the corresponding forbidden AG transition is strongly red-shifted and can participate in non-radiative decay of the excitation energy. This explains why “face-to-face” dimers are non-fluorescent. For the “slipped-stack” configurations with larger shifts (Δx), the allowed BU transition becomes red-shifted with an increasing dislocation and its energy drops below the corresponding AG forbidden transition. This explains why the “slipped-stack” and “edge-to-edge” dimers are fluorescent. The angle corresponding to zero splitting between BU and AG transitions is 54.7°, which is indicated by a vertical line in Fig. 6.

As it is seen from Fig. 6, there is a qualitative agreement between the TD-DFT results and equation (1). At the interplane distance of 3.5 Å, the energy splitting depends on the shift unevenly due to short-range effects of MO overlap (see below). These effects become negligible already at the 4.0 Å distance. For the edge-to-edge arrangement (Δz = 0), the center-to-center distances r < 16 Å are not possible which results in a very small excitonic splitting in agreement with eq. (1). For “planar” dimer 2 this distance is 15.7 Å, and the predicted excitonic splitting is small. Thus, the near-zero redshift in edge-to-edge dimers 1 and 2 is simply explained by a large distance between transition dipole centres. However, there is no quantitative agreement between TD-DFT transition energies and eq. (1) which can be further explained by short-range effects of π-MO overlap [36-40] (see below).

Distance dependence. As shown by Harcourt et al. [46] the excitonic interactions can be divided into long-range Coulomb interactions, Dexter's short-range exchange [47] and superexchange interactions caused by the -MO overlap [40]. Taking into account only Coulomb interactions leads to the Kasha exciton model [22], often approximated as a point-dipole interaction (eq. 1) that decays as 1/r3, whereas the superexchange interaction depends on the MO overlap that decays exponentially with distance.

Fig. 7. Distance dependence of the TD-DFT Q-band splitting in the face-to-face ZnPc dimer Non-uniform x axis? Units?

To exclude the influence of the variable MO overlap, only perfect face-to-face and edge-to-edge arrangements were considered to study the distance dependence of the excitonic Q-band splitting. As it is seen from Fig. 7, at larger Δz distances the splitting dependence is almost linear against 1/r whereas from eq. (1) the proportionality expected is 1/r3. A more detailed treatment of the Coulomb component of the excitonic coupling has been performed using the atomic charges obtained from the transition electrostatic potential fitting (TrESP charges) [48]. At larger distances, TD-DFT transition energy (ΔE) for dimers is well reproduced by a Coulomb contribution (ΔECoul) from monomers' transition charges. The TrESP Coulomb component is linear against 1/r rather than against 1/r3, which can be explained by a short distance between the transition dipoles. Significant disagreement between the TD-DFT transition energy and the predicted Coulomb component (Fig. 7) at shorter interplane distances (Δz) indicates a large impact of the short-range effects on the excitonic coupling. Other noticeable effect is a non-symmetrical splitting at shorter distances (Fig. 2): the red shift of the AG transition is larger than the blue shift of the BU transition. This can be explained by a larger contribution of a lower-energy transition to the configuration of the excited state (Table S2). The red-shifted AG transition is forbidden, therefore H-aggregates show only a blue-shifted Q-band. In crystals, the red-shifted Q-band absorption component often extends beyond 800 nm whereas the blue-shifted band is usually observed at 600 – 650 nm. For edge-to-edge arrangement (Δz = 0), the TD-DFT Q-band splitting is only 0.06 eV at Δx = 17 Å, being purely Coulombic. Thus, moderate ~ 0.15 eV blue shift observed for H-aggregates is only a "tip of an iceberg", and the short-range intermolecular electronic interaction is much stronger than it can be expected from the experimental spectra. This can explain a well-known excited-state quenching in aggregated Pcs [11-13] and some properties of Pc-based molecular conductors [16] (since the short-range excitonic coupling is related to electron- and hole-transfer integrals [11, 40]).

MO analysis. The π-π MO overlap results in splitting of the HOMO and LUMO levels of the monomers as shown in Fig. 8. The HOMO and LUMO splitting pattern in the slipped-stack dimers is determined by the MO shapes of the corresponding monomers [36, 40]. The MO overlap is responsible for short-range effects (see above) often expressed as charge-resonance/charge-transfer (CR/CT) excitons [11, 40]. The MO overlap and, as a consequence, charge-transfer integrals[40, 49] are very sensitive to the intermolecular arrangement which results in a great variability of photophysical and electric properties  of crystalline modifications of phthalocyanines[1-3, 15, 40, 50].

Fig. 8. Dependence of the HOMO (a1u) and LUMO (egx) splitting for ZnPc dimers at Δz = 3.5Å on the shift (Δx)Units?

Energies of high-lying occupied (au, bg) and low-lying vacant (ag, bu) orbitals of the ZnPc dimers at Δz = 3.5Å and various shift values (Δx)

Fig. 9. Distance dependence of HOMO and LUMO splitting for face-to-face ZnPc dimers (Δx = 0)

Parallel shift between Pc molecules in the dimer results in oscillations of the split MO levels with different periodicity for HOMO and LUMO, as a result of different nodal patterns of the monomers’ HOMO and LUMO (Figs. 4, 8) [36]. The splitting generally decreases with the shift due to decreasing overall π-MO overlap. The dependence of the splitting on distance is exponential as a result of the exponential decay of π -MO overlap (Fig. 9). This is in contrast to the 1/r dependence of the TD-DFT transition energies at larger distances. Therefore, at distances > 4Å, where MO splitting becomes negligible, the TD-DFT transition energies still show a non-zero excitonic splitting as a result of Coulomb coupling of the monomers’ transition dipoles.

Size dependence. Previously, optical gaps of π-conjugated Zn(II) oligoPcs were extrapolated to a 1D-polyPc using a free-electron approximation (E vs. 1/N) [42] which is applicable for delocalized systems only [51]. For typical molecular crystals, orbital and optical gaps may differ significantly [52], therefore extrapolation of TD-DFT optical gaps of oligomers can be a better estimate to the optical gap of an infinite stack than the orbital gap directly calculated in periodic boundary conditions.

According to a simplified tight-binding model including only nearest-neighbour interactions [36, 37], the band dispersion (width of HOMO or LUMO band) for a N-meric stack is described by the following equation:

ΔE = ± 2J cos[π / (N + 1)], 		(2)

with coupling factor J being either JCoul or JCT for Coulomb or charge-transfer excitonic coupling, respectively. As it was shown by Bredas et al., the MO band edges are linear against cos[π / (N + 1)] for phthalocyanines and other molecular semiconductors [36]. Similar extrapolation was also applied for optical gaps of oligothiophenes [53].

The excitonic splitting of two Q-band transitions results in 2·N transitions for the N-meric ZnPc. The TD-DFT spectrum is dominated by two x- and y-oriented transitions (Aux and Auy, respectively, see Fig. 3) which corresponds to all monomers' transition dipoles (Fig. 5) pointing in the same direction. All other transitions are of zero or low intensity (f < 0. 02).

Equation (2) can be used to predict excitonic splitting of optical spectra for infinite stacks in crystals.

Fig. 10. Size dependence of main TD-DFT Q-band transition energies of slipped-stacked ZnPc oligomers (resembling β-ZnPc stacks) Definitions? N=?

To study size dependence of the excitonic splitting, larger aggregates (stacks) were calculated with the arrangements approximately resembling β-modification of ZnPc (translation vectors taken from the X-Ray structure [54]). As no single-crystal X-Ray structure is available for α-ZnPc, stacks with Δz of 3.3 – 3.4Å and Δx of 1.75 – 2.0Å along the Zn-N bond (Fig. 4A) were studied (the Zn–Zn distance 3.75 – 3.95 Å, the inclination angle 28 – 31°, see Fig. 2). The results are shown in Fig. 10 and Table S3. As it is seen from Fig. 10, the TD-DFT Q-band splitting is almost linear against cos[π/(N+1)] for N = 1…5 in agreement with eq. (2). This indicates that excitonic splitting of the Q-band is mainly determined by interactions with the nearest neighbours. The extrapolated to N = ∞ transition energies of 1.97 eV (630 nm) and 1.72 eV (720 nm) for a single stack of β-modification are close to the experimental values (Fig. 2) of 1.94 eV (640 nm) and 1.65 eV (750 nm). Oscillator strengths increase almost linearly with size (Fig. S3), the extrapolated ratio of 1:1.52 being also in agreement with the experimental spectrum (Fig. 2).  Our estimates of the Q-band splitting for α-ZnPc vary from 0.06 eV (23 nm) to 0.16 eV (55 nm) (Table S4), i.e. very small variations of the intermolecular arrangement result in significant changes of the Q-band splitting. This explains why Zn(II), Ni(II) and Cu(II) Pcs have different solid-state spectra despite very similar crystal structures [38].  The approximate agreement between extrapolated and experimental spectra of β-ZnPc confirms that crystal spectra are determined mainly by excitonic coupling within the stack. For more quantitative description, next-nearest-neighbour and inter-stack couplings should also be considered [38].

Conclusions

Excitonic coupling of the electronic transitions in a series of zinc(II) phthalocyanine dimers was studied by TD-DFT with a range-separated hybrid functional LC-BLYP. This method correctly reproduces the experimental excitonic shifts of the Q-band for known "rigid" non-conjugated binuclear phthalocyanines.

The near-zero expected excitonic redshift of the Q-band for the "edge-to-edge" Pc dimers is a result of a large distance between transition dipole centres (weak Coulomb coupling) and absence of the π-MO overlap (no short-range coupling). In contrast, slipped-stacked arrangement of the Pc rings in dimers and crystals results in strong redshifts of the Q-band due to the π-MO overlap and short-range excitonic coupling. The Kasha's point-dipole approximation (eq. (1)) is qualitatively applicable although the 1/r3 factor is actually a superposition of the 1/r factor for the Coulomb coupling and the e-r factor for the short-range interactions. Short-range excitonic coupling is highly sensitive to the intermolecular arrangement due to a complicated HOMO-LUMO nodal pattern which determines the bonding/antibonding character of the π-MO overlap.

The well-known ~ 50 nm (~ 0.15 eV) blue shift of the Q-band of the "face-to-face" Pc dimers (H-aggregates) is only a "tip of an iceberg": the red-shifted (by ~ 0.65 eV) forbidden subband is not observed in the optical spectra but such a strong excitonic coupling undoubtedly influences other important properties. The excitonic splitting of the Q-band can be extrapolated from Pc oligomers to an infinite 1D-stack, in the frame of the tight-binding approximation (eq. (2)). This approach can be further extended to include the next-nearest-neighbour and inter-stack couplings for predicting optical spectra of crystalline phthalocyanines.

Computational details

DFT calculations. Geometry optimizations and TD-DFT calculations were carried out as described previously [42]. Range-separated hybrid functional LC-BLYP (μ = 0.4) [55-57] with the def2-TZVP(-f)/def2-J [57-59] basis sets was used for TD-DFT calculations. All geometries were optimized using the B3PW91 functional [60, 61] and 6-31G(d) (6D, 7F) basis set [62-64]. DFT geometry optimizations were carried out by the Firefly 8.2.0 program [65] which is partially based on the GAMESS (US) [66], with  pruned grid (99, 590) and default convergence criteria. TD-DFT calculations were carried out by ORCA 6.0.1 [67], with the RIJCOSX approximation [68, 69], default grid “Defgrid2” and tight SCF convergence.

Transition charges were calculated by fitting the Q-band transition electrostatic potential (TrESP [48]) of the B3PW91-optimized ZnPc using the CHELPG scheme [70] as implemented in the Multiwfn 3.6.1 software [71].

Extrapolation of TD-DFT spectra was carried out for ZnPc stacks of the 2…5 size constructed from the B3PW91-optimized ZnPc molecules positioned either according to the translation vectors from β-ZnPc [54], or by applying shifts of Δx = 3.3 – 3.4Å, Δz = 1.75 – 2.0Å (Fig. 4A) to simulate the α-ZnPc stacks.

References

- D. Wöhrle, G. Schnurpfeil, S.G. Makarov, A. Kazarin, O.N. Suvorova, Macroheterocycles, 2012, 5, 191.

- N.B. McKeown, Phthalocyanine Materials, Cambridge University Press, 1998.

- P. Erk, H. Engelsberg, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 19, 105.

- B.H. Lessard, ACS Appl. Mater. Interfaces, 2021, 13, 31321.

- Z.J. Comeau, R.R. Cranston, H.R. Lamontagne, A.J. Shuhendler, B.H. Lessard, Commun. Chem., 2022, 5, 178.

- H. Kobayashi, P.L. Choyke, Acc. Chem. Res., 2019, 52, 2332

- S.G. Makarov, O.N. Suvorova, D. Wöhrle, J. Porphyrins Phthalocyanines, 2011, 15, 791.

- S.G. Makarov, G. Schnurpfeil, S.Yu. Ketkov, D. Wöhrle, J. Porphyrins Phthalocyanines, 2019, 24, 515.

- S.G. Makarov, G. Schnurpfeil, S.Yu. Ketkov, D. Wöhrle, J. Porphyrins Phthalocyanines, 2021, 25, 236.

- N. Kobayashi, Coord. Chem. Rev., 2002, 227, 129.

- K. Ishii, N. Kobayashi, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 16, 1.

- K. Kameyama, M. Morisue, A. Satake, Y. Kobuke, Angew. Chem. Int. Ed. 2005, 44, 4763

- A.W. Snow, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 17, 129.

- M. J. Cook, I. Chambrier, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 17, 37.

- M. K. Engel, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 20, 1.

- T. Inabe, H. Tajima, Chem. Rev., 2004, 104, 5503.

- M. Hanack, D. Dini, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 18, 251.

- K. Ishii, N. Kobayashi, M. Fujitsuka, S. Abiko and O. Ito, J. Chem. Soc., Dalton Trans., 2002, 1735

- M. V. Martinez-Diaz, M. S. Rodriguez-Morgade, M. C. Feiters, P. J. M. van Kan, R. J. M. Nolte, J. F. Stoddart, T. Torres, Org. Lett., 2000, 2, 1057.

- A. Escosura, M. V. Martinez-Diaz, P. Thordarson, A. E. Rowan, R. J. M. Nolte, T. Torres, J. Am. Chem. Soc., 2003, 125, 12300.

- A. Davydov, Theory of Molecular Excitons, Springer, New York, 2013.

- M. Kasha, H. R. Rawls, M. A. El-Bayoumi, Pure Appl. Chem. 1965, 11, 371.

- H. Eichhorn, D. Wöhrle, D. Pressner, Liq. Cryst. 1997, 22, 643.

- Tolbin A.Yu., Tomilova L.G., Zefirov N.S. Russ. Chem. Rev. 2008, 77, 435-449

- A.G. Martynov, Yu.G. Gorbunova, A.Yu. Tsivadze, Russian J. Inorg. Chem., 2014, 59, 1635.

- N. Kobayashi, H. Lam, W.A. Nevin, P. Janda, C.C. Leznoff, A.B.P. Lever, Inorg. Chem. 1990, 29, 3415.

- Y. Yamada, T. Maeno, K. Nawate and K. Tanaka, Chem. Commun., 2018, 54, 8226.

- S.G. Makarov, K.N. Maksimova, E.V. Baranov, G.K. Fukin, O. N. Suvorova, D. Wöhrle, G.A. Domrachev, Russ. Chem. Bull., 2006, 55, 1748.

- Y. Asano, M. Uchiyama, A. Fukasawa, T. Hatano, A. Muranaka and N. Kobayashi, J. Am. Chem. Soc., 2007, 129, 4516.

- Y. Asano, J. Sato, T. Furuyama, N. Kobayashi, Chem. Commun., 2012, 48, 4365

- L. Zhao, X. Ren, X. Yan, CCS Chem. 2021, 3, 678.

- J.E. Norton, J.-L. Bredas, J. Chem. Phys., 2008, 128, 034701.

- B.L. Wheeler, G. Nagasubramanian, A.J. Bard, L.A. Schechtman, D.R. Dininny, M.E. Kenney, J. Am. Chem. Soc. 1984, 106, 7404.

- G. De La Torre, A. Hausmann, M. Sekita, G. Bottari, T. Torres and D. M. Guldi, Chem. Soc. Rev., 2013, 42, 8049.

- T. Mirkovic, R. Van Grondelle, E.E. Ostroumov, J.M. Anna, G. Govindjee, G.D. Scholes, Chem. Rev. 2017, 117, 249.

- J. L. Bredas, D. A. Da Silva Filho, J. Cornil and J. P. Calbert, PNAS, 2002, 99, 5804

- S. Yanagisawa, I. Hamada, K. Yamauchi, T. Oguchi and T. Inaoka, Phys. Rev. B, 2014, 90, 245141.

- L. P. Doctor, F. Ziegs, B. Büchner, M. Naumann, A. Popov and M. Knupfer, J. Phys. Chem. C, 2021, 125, 12398.

- M. Kato, J. Onoe, Y. Matoba, K. Okamoto, S. Watanabe, J.-P. Bucher, M. Nakaya, J. Chem. Phys., 2020, 153, 144704.

- N.J. Hestand, F.C. Spano, Acc. Chem. Res., 2017, 50, 341.

- A.O. Gudovannyy, J.M. Schäfer, O. Gerdes, D. Hildebrandt, G. Mattersteig, M. Pfeiffer, F. Ortmann, Adv. Funct. Mater. 2025, 2421048

- S. G. Makarov, G. Schnurpfeil, S. Y. Ketkov and D. Wöhrle, J. Porphyrins Phthalocyanines, 2020, 24, 515.

- S. G. Makarov, S. Y. Ketkov, D. Wöhrle and G. Schnurpfeil, Journal of Porphyrins and Phthalocyanines, 2021, 25, 236

- J.P. Heindel, K.M. Herman, E. Apra, S.S. Xantheas, J. Phys. Chem. Lett., 2021, 12, 7574

- H. Isago, Optical Spectra of Phthalocyanines and Related Compounds, Springer, Japan, 2015.

- R. D. Harcourt, G. D. Scholes, K. P. Ghiggino and S. Speiser, J. Chem. Phys., 1996, 105, 1897.

- D.L. Dexter J. Chem. Phys. 1953, 21, 836.

- T. Renger, F. Müh, Photosynth. Res., 2012, 111, 47.

- P.M. Kazmaier, R. Hoffmann, J. Am. Chem. Soc. 1994, 116, 9684-9691.

- H. Jiang, Y. Li, C. Kloc, J. Ye, Y. Long, D. Fichou, W. Hu, R. Ganguly ,P. Hu, Angew. Chem. Int. Ed. 2018, 57, 10112.

- J. Torras, C. Aleman, J. Casanovas, J. Phys. Chem. A, 2012, 116, 7571.

- J.-L. Bredas, Mater. Horiz., 2014, 1, 17.

- R.E. Larsen, J. Phys. Chem. C, 2016, 120, 9650.

- W.R. Scheidt, W. Dow, J. Am. Chem. Soc., 1977, 99, 1101.

- A. D. Becke, Phys. Rev. A, 1988, 38, 3098.

- C. Lee, W. Yang, R. G. Parr, Phys. Rev. B, 1988, 37, 785.

- H. Iikura, T. Tsuneda, T. Yanai, K. Hirao, J. Chem. Phys., 2001, 115, 3540.

- F. Weigend, R. Ahlrichs, Phys. Chem. Chem. Phys., 2005, 7, 3297.

- F. Weigend, Phys. Chem. Chem. Phys., 2006, 8, 1057.

- A.D. Becke, J. Chem. Phys., 1993, 98, 5648.

- J.P. Perdew, Y. Wang, Phys. Rev. B, 1992, 45, 13244.

- W.J. Hehre, R. Ditchfield, J.A. Pople, J. Chem. Phys., 1972, 56, 2257.

- P.C. Hariharan, J.A. Pople, Theor. Chem. Acc., 1973, 28, 213.

- V. A. Rassolov, J. A. Pople, M. A. Ratner, T. L. Windus, J. Chem. Phys., 1998, 109, 1223.

- A.A. Granovsky, Firefly version 8.2.0, www http://classic.chem.msu.su/gran/firefly/index.html

- M.W. Schmidt, K.K. Baldridge, J.A. Boatz, S.T. Elbert, M.S. Gordon, J.H. Jensen, S. Koseki, N. Matsunaga, K.A. Nguyen, S.J. Su, T.L. Windus, M. Dupuis, J. A. Montgomery, J. Comput. Chem., 1993, 14, 1347.

- F. Neese, Wiley Interdiscip. Rev.: Comput. Mol. Sci., 2025, 15, e70019.

- B.I. Dunlap, J. Chem. Phys., 1983, 78, 3140.

- F. Neese, F. Wennmohs, A. Hansen and U. Becker, Chem. Phys., 2009, 356, 98.

- C.M. Breneman, K.B. Wiberg, J. Comput. Chem., 1990, 11, 361.

- T. Lu and F. Chen, J. Comput. Chem., 2012, 33, 580.