Excitonic coupling of electronic transitions in oligomeric phthalocyanine zinc(II) complexes

Sergei G. Makarov*a, Sergey Yu. Ketkova and Dieter Wöhrleb

aG.A. Razuvaev Institute of Organometallic Chemistry of RAS, Tropinin str. 49, 603950 Nizhniy Novgorod, Russia

bUniversität Bremen, Institut für Angewandte und Physikalische Chemie, P.O. Box 330440, 28334 Bremen, Germany

Received

Accepted

ABSTRACT:

KEYWORDS: phthalocyanines, oligophthalocyanines, electronic transitions, excitonic coupling, time-dependent DFT

*Correspondence to: Sergei G. Makarov, email: makar@iomc.ras.ru

Introduction

Phthalocyanines (Pc) have found many “real” applications as colorants and in electronic devices [1-3]. Successful practical use of phthalocyanines (Pcs) in many fields became possible due to their unique structural diversity of the molecules, photophysical properties and different arrangements in the solid state. Recent potential applications include organic thin-film transistors [4, 5], near-infrared fluorescent diagnostics and photodynamic immunotherapy [6] of tumors.

Photophysical properties of phthalocyanine metal complexes can be modified by peripheral substituents, central metal ions or by extension of the π-system [7-9]. The extended π-system of conjugated Pc oligomers results in large redshifts of the lowest-energy absorption (Q-band). Noncovalent interactions (excitonic coupling) of the Pc π-systems are also known to significantly influence photophysical properties of phthalocyanines in aggregates, non-conjugated dimers and crystals [10-34].

Non-conjugated oligo- and polymeric phthalocyanine assemblies include well-known π-π stacked aggregates in solution [13] and in the solid state [2, 3, 14-15]. Besides, non-conjugated oligomers via ligand [10, 23-30, 34], metal–ligand [12, 14, 17, 18, 25], hydrogen-bonded [19] and donor-acceptor systems [20] have also been reported.

Two types of arrangement of chromophore molecules in aggregates are usually discussed: face-to-face configurations, often referred as H-type aggregates, and edge-to-edge or slipped-stacked configurations known as J-type aggregates (Fig. 1) [13]. A close proximity of the chromophores causes excitonic coupling of their electronic transitions, which significantly influences their photophysical properties [11, 21-22].

According to Kasha’s theory [22], “face-to-face” molecular dimers (H-aggregates) exhibit a blue-shifted absorption maximum and a suppressed radiative decay rate. In contrast “edge-to-edge” and “slipped-stacked” dimers (J-aggregates) exhibit a red-shifted absorption maximum and an enhanced radiative decay rate. For dimers with parallel arrangement of chromophores, the interaction of the transition dipoles can be approximated by a simple point-dipole model as described by Eq. 1.

∆E≈μ2(1-3cos2θ)4πεr3	(1)

In Eq. 1 μ and r represent the magnitude of the transition moment in the monomer and the center-to-center distance between the molecules, respectively. θ is the angle between the polarization axis and the line between the dipole centers. The energy change ΔE becomes zero at θ = 54.7°, i.e. two molecules behave as an H-aggregate above θ = 54.7° and as a J-aggregate below this angle.

Fig. 1. Excitonic coupling of electronic transitions in molecular dimers

Although many examples of "face-to-face" phthalocyanine dimers, oligomers and aggregates [10, 23-27, 33-34] and a few "edge-to-edge" and "slipped-stack" dimers and aggregates were described [12, 17, 28-31]. But the exact alignment of the Pc subunits in these systems is not known, except for the crystals where slipped-stacked arrangement is typical for M(II)Pcs [1, 2, 15, 16]. Only a few binuclear Pcs with a linker rigid enough to ensure a well-defined geometry are known experimentally (Chart 1): a “gable” 1 [32], a “planar” 2 [30], a “cyclophane” 3 [31] bridged binuclear phthalocyanines with “edge-to-edge” und a “slipped-stack” arrangement (J-dimers). For “face-to-face” binuclear Pcs (H-dimers) with rigid linkers such as 4 [26] and 5 [27] different conformations are still possible with significantly different excitonic coupling (see below). One example of a supramolecular dimer 6 [12] can be considered rigid although two configurations (“parallel” and “oblique”) are possible.

Fig. 2. Electronic spectra and crystal packing of α- and β-modifications of ZnPc [1] Please mention Fig.2 in the text

The effect of aggregation on the Q-band in solution is stronger than solvent effects. This typically results in a blue shift from = 660 - 700 nm and = 600 - 640 nm with broadening of the Q-band (H-aggregates) [13]. Similar blue shifts were observed for various covalent and supramolecular cofacial dimers [10, 12, 24-27, 33-34]. In the solid state, β-modification of planar M(II)Pcs typically shows a close contact of central metal ion to a meso-N atom of an adjacent molecule in the stack and an inclination angle of the macrocycles within the stack of ~45°. The inclination angle in α-modification is ~30°, and the metal shows a close contact to a pyrrole-N atom of an adjacent molecule. Different arrangements of chromophores result in a significantly different excitonic coupling. This leads to a high variability of absorption wavelengths by crystalline phthalocyanines. Thus, α-modifications of CuPc and ZnPc absorb at λ ~625 and ~700 nm, β -modifications at λ ~650 and ~750 nm, and ε-CuPc exhibits an absorption at even longer wavelength at λ <820 nm [1-3]. The non-planar Ti(O)Pc with slipped-stacked arrangement similar to J-aggregates shows an extremely red-shifted Q-band absorption at λ ~700 - 900 nm and an efficient photoinduced charge carrier generation [32].

Slipped-stacked Pc oligomers resemble structural patterns of photosynthetic light-harvesting antenna consisting of bacteriochlorophyll dimers [35], and they are photoactive in contrast to face-to-face Pc oligomers [11, 12, 36] for which a non-radiative decay of the excited states is typical. Therefore, edge-to-edge dimers and J-aggregates are highly desirable to tailor the photophysical properties of Pcs. The cyclophane-fused dimer 3 is fluorescent (Φf = 0.12), a metal-free “gable” dimer 1 is also fluorescent (Φf = 0.55), and a “planar” dimer 2 shows a singlet oxygen quantum yield of ΦΔ = 0.08. The imidazole-bridged supramolecular dimer 6 is also fluorescent (Φf = 0.26). Surprisingly, for edge-to edge Pc dimer 2 no redshift expected according to Kasha’s theory and the Eq. (1) was observed in contrast to slipped-stack 3 showing a strong bathochromic Q-band shift (Table 1), and H-dimers showing a significant hypsochromic shift. It was concluded [8, 31] that the π-MO overlap is essential for an efficient excitonic coupling in Pc dimers, crystals and aggregates. Purely Coulombic coupling of the transition dipoles (Eq. (1)) is not enough to explain the observed Q-band shifts. Short-range excitonic coupling in phthalocyanine dimers [36-38] and crystals [36-39] were studied previously by DFT and semi-empirical methods. It was shown that the short-range coupling is very sensitive to the MO overlap, which is related to electron- and hole-transfer integrals [40]. However, a more systematic study including various arrangements (r and θ) are required to provide a general explanation of the observed excitonic coupling effects in phthalocyanine oligomers and crystals.

To organize chromophores into tailored structures it is important to predict their photophysical properties. Nowadays, machine-learning methods are growing up for predicting crystal structures of molecular materials [41], which requires an accurate theoretical description of the intermolecular properties. Previously, we have studied UV/Vis/NIR spectra and energy gaps of conjugated oligomeric phthalocyanine zinc (II) complexes by TD-DFT. It was shown that calculations with range-separated hybrid functional LC-BLYP provide a good agreement with the experimental spectra [8,9]. The extrapolated TD-DFT Q-band energy of oligoPcs was compared to a directly calculated band gap of 1D-polyPc.

Here, we benchmark the above-mentioned LC-TDDFT approach on excitonically coupled Q-band transitions in non-conjugated binuclear ZnPcs for the first time. Then we use the same method to investigate the influence of the relative position of ZnPc molecules (r and θ in the Eq. (1)) on the Q-band transition energies, and finally to explain excitonic coupling effects observed for phthalocyanine aggregates, dimers and crystals.

Results and discussion

Bridged oligophthalocyanines. “Rigid” binuclear Pcs 1 – 3 and 6 were selected to exclude the influence of noncovalent interactions (poorly described by DFT [44]) on the relative position of the Pc chromophores.

| 1 (1a with substituents) | 2 (2a with substituents) |
| --- | --- |
| 3 (3a with substituents) | 4a |
| 5a (substituents omitted) | 6 (6a with substituents) |

Chart 1. "Rigid" ZnPc dimers

The calculated Q-band wavelengths and energies for the dimers 1 – 3, 6 without peripheral substituents are compared to experimental wavelengths of their Q-band maxima. The results are listed in the Table 1.

To include in Table 1 also References when described in the literature?

Table 1. Q-band wavelengths and energies for rigid non-conjugated oligoPcs 1 – 3, 6 and their substituted analogues 1a – 3a, 6a

| Cpd. # | Experimental (1a – 3a, 6a) |  | Theoretical (1 – 3, 6) |  |
| --- | --- | --- | --- | --- |
|  | λ, nm (ΔE, eV) | 10-5 ε, M-1·cm-1 | λ, nm (ΔE, eV) | Oscillator strength |
| ZnPc | 674 (1.840) | 3.4 | 685 (1.809) | 0.484 × 2 |
| 1, 1a | 694 (1.787) | 2.9 | 713 (1.738) | 1.050 |
|  | 677 (1.832) | 3.1 | 680 (1.823) | 0.906 |
| 2, 2a | 682 (1.818) | 6.9 | 705 (1.758) | 1.334 |
|  |  |  | 692 (1.790) | 0.912 |
| 3, 3a | 753 (1.647) | 0.84 | 743 (1.667) | 1.276 |
|  | 690 (1.797) | 0.72 | 688 (1.800) | 0.833 |
| 6, 6a | 700 (1.771) | 1.7 | 723 (1.714) | 1.070 |
| (parallel) | 670 (1.851) | 1.2 | 676 (1.832) | 0.749 |

As it is seen from the Table 1 theoretical wavelengths are relatively well in agreement with the experimental ones. Therefore TD-DFT with a range-separated hybrid functional LC-BLYP correctly predicts the through-space excitonic coupling of the excited states of ZnPcs. For edge-to-edge arrangements in 1 and 2 the redshift compared to the monomeric ZnPc and expected from Eq. (1) is negligible. This is in contrast to a well-known blue shift for face-to-face arrangements in H-dimers and aggregates [10-12, 24-27, 33-34]. In contrast, for the cyclophane-type dimer 3, a significant red shift and a splitting of the Q-band is apparent both theoretically and experimentally. The practical absence of the red shift predicted by Kasha’s theory for edge-to-edge dimers 1 and 2 was explained previously [8, 29] by the absence of π-π overlap and intermolecular π-electron delocalization. Thus, it is important to study whether a general Coulombic dipole-dipole model (Eq. (1)) is applicable for oligoPc. Or the observed excitonic coupling in phthalocyanine aggregates, dimers and crystals is a system-specific short-range effect determined by the π-π overlap.

Excitonic coupling between phthalocyanine molecules. To evaluate excitonic coupling effects in oligoPcs, model zinc phthalocyanine dimers with face-to-face, slipped-stacked and edge-to-edge parallel arrangements of the Pc rings with parallel shifts (Δx) from 0 to 20 Å and interplane distances (Δz) from 0 to 6 Å were studied by TD-DFT. The corresponding distances (r) and angles (θ) can be easily calculated to compare TD-DFT transition energies to those predicted by the Eq. (1). Pcs show intense π → π* transitions in the visible region of the absorption spectra. The Q-band transition originates from the doubly degenerate HOMO (a1u) → LUMO (eg) transition (Fig. 3) [45]. For a Pc dimer, there are four Q-band transitions arising from the excitonic splitting of two degenerate EU transitions of a single Pc chromophore: an allowed BU transition oriented in the shift direction (x) and AU in the perpendicular direction (y), both having oscillator strengths f ≈ 0.5, and two forbidden transitions AG and BG with f ≈ 0 corresponding to the opposite orientation of the monomers’ transition dipoles (Fig. 5). MOs of Pc oligomers can be approximately described as linear combinations of the monomers’ MOs [11, 12]. Due to the π-π overlap, the bonding-antibonding interactions between these MOs result in splitting of the corresponding energy levels and for infinite stacks to the formation of valence and conduction bands [36, 40]. The dependence of these energies on the arrangement of the Pc molecules (see Fig. 4) is shown in Fig. 6 for shift direction along Zn-N bond (Fig. 4A, approx. resembles stack arrangement in α-ZnPc). The corresponding transition energies are listed in Table S1. For shift direction along meso-N – Zn (Fig. 4B, approx. resembles stack arrangement in β-ZnPc) the results are shown in Fig. S1 and Table S2.

Fig. 3. Frontier MOs of ZnPc (front and side views)

Fig. 4. Arrangements of the monomers in slipped-stacked ZnPc dimers

Fig. 5. Frontier MO splitting and Q-band transitions in slipped-stacked ZnPc dimers

Fig. 6. TD-DFT Q-band transition energies vs. parallel shifts (Δx) between Pc molecules (arrangement in Fig. 4A). Forbidden transitions are shown by dashed lines

Angle dependence. For parallel transition dipoles the dependence of the excitonic splitting on the angle θ (Fig. 2) is approximately described by the Eq (1). With “face-to-face” arrangement the allowed X-oriented BU transition is blue-shifted in contrast the corresponding forbidden AG transition which is strongly red-shifted and can participate in non-radiative decay of the excitation energy. This explains why “face-to-face” dimers are non-fluorescent. For “slipped-stack” configurations with larger shifts (Δx) the allowed BU transition becomes red-shifted with increasing shift and its energy drops below the corresponding AG forbidden transition. This explains why “slipped-stack” and “edge-to-edge” dimers are fluorescent. The angle corresponding to zero splitting between BU and AG transitions corresponds to the angle of 54.7°, which is indicated by a vertical line in the Fig. 6.

As it is seen from the Fig. 6 there is a qualitative agreement between the TD-DFT which is in agreement with equation (1). At the 3.5 Å interplane distance the energy splitting dependence on the shift is nonuniform due to a short-range effects of the MO overlap (see below). These effects become negligible already at the 4.0 Å distance. For edge-to-edge arrangement (Δz = 0) the center-to-center distances r less than 16 Å are not possible which results in a very small excitonic splitting which is in agreement wih Eq. (1). For “planar” dimer 2 this distance is 15.7 Å, and the predicted excitonic splitting is small. Thus, the near-absence of the redshift in edge-to-edge dimers 1 and 2 is simply explained by a large distance between transition dipole centres.

However, there is no quantitative agreement between TD-DFT transition energies and Eq. (1) which can be further explained by short-range effects of the π-MO overlap [36-40] (see below).

Distance dependence. As shown by Harcourt et al. [46] the excitonic interactions can be divided into long-range Coulombic interactions, Dexter's short-range exchange [47] and superexchange interactions derived from the pi-MO overlap [40]. Retaining only the Coulombic interactions leads to Kasha’s exciton model [22] often approximated as a point-dipole interaction (equation 1). This decays as 1/r3 whereas superexchange interaction depends on the MO overlap which decays exponentially with the distance.

Fig. 7. Distance dependence of the TD-DFT Q-band splitting of a face-to-face ZnPc dimer

To exclude the fluence of the variable MO overlap, only perfect face-to-face and edge-to-edge arrangements were considered in order to study the distance dependence of the excitonic Q-band splitting. As it is seen from the Fig. 7, at larger Δz distances the splitting dependence is almost linear against 1/r whereas 1/r3 is expected from the Eq. (1). A more detailed treatment of the Coulombic component of the excitonic coupling has been made using atomic charges obtained from the transition electrostatic potential fitting (TrESP charges) [48]. At larger distances the TD-DFT transition energy (ΔE) for dimers is well reproduced by a Coulombic interaction (ΔECoul) of monomers' transition charges. The TrESP Coulombic component is linear against 1/r rather than 1/r3, which can be explained by a short distance between the transition dipoles. Significant disagreement of the TD-DFT transition energy and the predicted Coulombic component (Fig. 7) at shorter interplane distances (Δz) indicates a large impact of short-range effects on the excitonic coupling. Another noticeable effect is a non-symmetrical splitting at shorter distances (Fig. 2): the red shift of the AG transition is larger than the blue shift of the BU transition. This can be explained by a larger contribution of a lower-energy transition in the configuration of the excited state (Table S2). The red-shifted AG transition is forbidden, therefore H-aggregates only show a blue-shifted Q-band. In crystals, the red-shifted Q-band absorption component often extends beyond = 800 nm whereas the blue-shifted band is usually observed at = 600 – 650 nm. For the edge-to-edge arrangement (Δz = 0), the TD-DFT Q-band splitting is only 0.06 eV at Δx = 17 Å and is purely Coulombic. Thus, a moderate ~ 0.15 eV blue shift observed for H-aggregates is only a "tip of an iceberg". The short-range intermolecular electronic interaction is much stronger than it can be expected from the experimental spectra. This can explain a well-known excited-state quenching in aggregated Pcs [11-13] and some properties of Pc-based molecular conductors [16] (since a short-range excitonic coupling is related to electron- and hole-transfer integrals [11, 40]).

MO analysis. The π-π MO overlap results in splitting of HOMO and LUMO levels of the monomers as shown in the Fig. 8. HOMO and LUMO splitting pattern in the slipped-stack dimers is determined by a shape of the corresponding monomers’ orbitals [36, 40]. The MO overlap is responsible for short-range effects (see above) often expressed as charge-resonance/charge-transfer (CR/CT) excitons [11, 40]. The MO overlap and, as a consequence, the charge-transfer integrals [40, 49] are very sensitive to an intermolecular arrangement which results in a great variability of photophysical and electric properties [1-3, 15, 40, 50] of crystalline modifications of phthalocyanines.

Fig. 8. Shift (Δx) dependence of HOMO (a1u) and LUMO (egx) splitting for ZnPc dimers at Δz = 3.5Å

Fig. 9. Distance dependence of HOMO and LUMO splitting for face-to-face ZnPc dimers (Δx = 0)

A parallel shift between Pc molecules in the dimer results in oscillations of the split MO levels with different periodicity for HOMO and LUMO which is a result of different nodal patterns of the monomers’ HOMO and LUMO (see Fig. 8, Fig. 4) [36]. The splitting generally decreases with the shift due to decreasing overall π-MO overlap. The distance dependence of the splitting is exponential as a result of the exponential decay of the π -MO overlap (Fig. 9). This is in contrast to the 1/r dependence of the TD-DFT transition energies at larger distances. Therefore, at distances > 4Å where MO splitting becomes negligible. The TD-DFT transition energies still show a non-zero excitonic splitting as result of Coulombic coupling of the monomers’ transition dipoles.

Size dependence. Previously optical gaps of π-conjugated Zn(II) oligoPcs were extrapolated to a 1D-polyPc using a free-electron approximation (E vs. 1/N) [42] which is only applicable for delocalized systems [51]. For typical molecular crystals orbital and optical gaps may differ significantly [52]. Therefore, extrapolation of TD-DFT optical gaps of oligomers can be a better estimate to the optical gap of an infinite stack than the orbital gap directly calculated in periodic boundary conditions.

According to a simplified tight-binding model including only the nearest-neighbour interactions [36, 37], with ??? the band dispersion (width of HOMO or LUMO band) for a N-meric stack is described by the following Eq. (2).

ΔE = ± 2J cos[π / (N + 1)], 		(2)

The coupling factor J is either JCoul or JCT for Coulombic or charge-transfer excitonic coupling, respectively. As it was shown by Bredas et al., the MO band edges are linear against cos[π / (N + 1)] for phthalocyanines and other molecular semiconductors [36]. Similar extrapolation was also applied for optical gaps of oligothiophenes [53].

The excitonic splitting of two Q-band transitions results in 2·N transitions for the N-meric ZnPc. The TD-DFT spectrum is dominated by two x- and y-oriented transitions (Aux and Auy, respectively, see Fig. 3) which corresponds to all monomers' transition dipoles (Fig. 5) pointing in the same direction. All other transitions are of zero or low intensity (f < 0. 02).

The equation (2) can be used to predict the excitonic splitting of optical spectra for infinite stacks in crystals.

Fig. 10. Size dependence of main TD-DFT Q-band transition energies of slipped-stacked ZnPc oligomers (comparable β-ZnPc stacks)

To study the size dependence of the excitonic splitting, larger aggregates (stacks) were calculated with the arrangements approximately resembling the β-modification of ZnPc (translation vectors taken from the X-Ray structure [54]). As no single-crystal X-Ray structure is available for α-ZnPc, stacks with Δz of 3.3 – 3.4Å and Δx of 1.75 – 2.0Å along Zn-N bond (Fig. 4A) were studied (Zn–Zn distance 3.75 – 3.95 Å, inclination angle 28 – 31°, see Fig. 2). The results are shown in Fig. 10 and Table S3. As it is seen from Fig. 10, the TD-DFT Q-band splitting is almost linear against cos[π/(N+1)] for N = 1…5 which is in agreement with equation (2). This indicates that excitonic splitting of the Q-band is mainly determined by nearest-neighbour interactions. The extrapolated to N = ∞ transition energies of 1.97 eV (630 nm) and 1.72 eV (720 nm) for a single stack of β-modification are close to the experimental values (Fig. 2) of 1.94 eV (640 nm) and 1.65 eV (750 nm). Oscillator strengths increase almost linearly with size (Fig. S3) and with the extrapolated ratio of 1:1.52 which is also in agreement with the experimental spectrum (Fig. 2). Our estimates of the Q-band splitting for α-ZnPc vary from 0.06 eV (23 nm) to 0.16 eV (55 nm) (Table S4), i.e. very small changes of the intermolecular arrangement result in significant changes of the Q-band splitting. This explains why Zn(II), Ni(II) and Cu(II) Pcs have different solid-state spectra despite very similar crystal structures [38]. The approximate agreement between extrapolated and experimental spectra of β-ZnPc confirms that crystal spectra are determined mainly by excitonic coupling within the stack. For a more quantitative description, the next-nearest-neighbour and the inter-stack couplings should also be considered [38].

Conclusions

Excitonic coupling of the electronic transitions in a series of zinc(II) phthalocyanine dimers was studied by TD-DFT with a range-separated hybrid functional LC-BLYP. This method correctly reproduces the experimental excitonic shifts of the Q-band for known "rigid" non-conjugated binuclear phthalocyanines.

The near-absence of the expected excitonic redshift of the Q-band for "edge-to-edge" Pc dimers is a result of a large distance between transition dipole centres (weak Coulombic coupling) and absence of the π-MO overlap (no short-range coupling). In contrast, the slipped-stacked arrangement of the Pc rings in dimers and crystals results in a strong redshift of the Q-band due to the π-MO overlap and the short-range excitonic coupling.

The Kasha's point-dipole approximation (eq. (1)) is qualitatively applicable although 1/r3 is actually a superposition of 1/r for Coulombic coupling and e-r for short-range coupling.

The short-range excitonic coupling is highly sensitive to the intermolecular arrangement due to a complicated HOMO-LUMO nodal pattern which determines the bonding/antibonding character of the π-MO overlap.

The well-known ~ 50 nm (~ 0.15 eV) blue shift of the Q-band of "face-to-face" Pc dimers (H-aggregates) is only a "tip of an iceberg": the red-shifted (by ~ 0.65 eV) forbidden subband is not observed in the optical spectra but such a strong excitonic coupling undoubtedly influences other important properties.

The excitonic splitting of the Q-band can be extrapolated from Pc oligomers to an infinite 1D-stack, in the frame of the tight-binding approximation (Eq. (2)). This approach can be further extended to include the next-nearest-neighbour and the inter-stack couplings for predicting optical spectra of crystalline phthalocyanines.

Computational details

DFT calculations. Geometry optimizations and TD-DFT calculations were carried out as described previously [8]. Range-separated hybrid functional LC-BLYP (μ = 0.4) [55-57] with def2-TZVP(-f)/def2-J [57-59] basis sets was used for TD-DFT calculations. All geometries were optimized using B3PW91 functional [60, 61] and 6-31G(d) (6D, 7F) basis set [62-64]. DFT geometry optimizations were carried out by the Firefly 8.2.0 program [65] which is partially based on the GAMESS (US) [66], with (99, 590) pruned grid and default convergence criteria. TD-DFT calculations were carried out by ORCA 6.0.1 [67], with RIJCOSX approximation [68, 69], default grid “Defgrid2” and tight SCF convergence.

Transition charges were calculated by fitting the Q-band transition electrostatic potential (TrESP [48]) of B3PW91-optimized ZnPc using CHELPG scheme [70] as implemented in Multiwfn 3.6.1 software [71].

Extrapolation of TD-DFT spectra was carried out for ZnPc stacks of 2…5 size constructed from B3PW91-optimized ZnPc molecules positioned either according to translation vectors from β-ZnPc [54] or by applying shifts of Δx = 3.3 – 3.4Å, Δz = 1.75 – 2.0Å (Fig. 4A) to simulate α-ZnPc stacks.

References

- D. Wöhrle, G. Schnurpfeil, S.G. Makarov, A. Kazarin, O.N. Suvorova, Macroheterocycles, 2012, 5, 191.

- N.B. McKeown, Phthalocyanine Materials, Cambridge University Press, 1998.

- P. Erk, H. Engelsberg, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 19, 105.

- B.H. Lessard, ACS Appl. Mater. Interfaces, 2021, 13, 31321.

- Z.J. Comeau, R.R. Cranston, H.R. Lamontagne, A.J. Shuhendler, B.H. Lessard, Commun. Chem., 2022, 5, 178.

- H. Kobayashi, P.L. Choyke, Acc. Chem. Res., 2019, 52, 2332

- S.G. Makarov, O.N. Suvorova, D. Wöhrle, J. Porphyrins Phthalocyanines, 2011, 15, 791.

- S.G. Makarov, G. Schnurpfeil, S.Yu. Ketkov, D. Wöhrle, J. Porphyrins Phthalocyanines, 2020, 24, 515.

- S.G. Makarov, G. Schnurpfeil, S.Yu. Ketkov, D. Wöhrle, J. Porphyrins Phthalocyanines, 2021, 25, 236.

- N. Kobayashi, Coord. Chem. Rev., 2002, 227, 129.

- K. Ishii, N. Kobayashi, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 16, 1.

- K. Kameyama, M. Morisue, A. Satake, Y. Kobuke, Angew. Chem. Int. Ed. 2005, 44, 4763

- A.W. Snow, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 17, 129.

- M. J. Cook, I. Chambrier, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 17, 37.

- M. K. Engel, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 20, 1.

- T. Inabe, H. Tajima, Chem. Rev., 2004, 104, 5503.

- M. Hanack, D. Dini, in The Porphyrin Handbook, ed. K. M. Kadish, K. M. Smith and R. Guilard, Academic Press, San Diego, 2003, 18, 251.

- K. Ishii, N. Kobayashi, M. Fujitsuka, S. Abiko and O. Ito, J. Chem. Soc., Dalton Trans., 2002, 1735

- M. V. Martinez-Diaz, M. S. Rodriguez-Morgade, M. C. Feiters, P. J. M. van Kan, R. J. M. Nolte, J. F. Stoddart, T. Torres, Org. Lett., 2000, 2, 1057.

- A. Escosura, M. V. Martinez-Diaz, P. Thordarson, A. E. Rowan, R. J. M. Nolte, T. Torres, J. Am. Chem. Soc., 2003, 125, 12300.

- A. Davydov, Theory of Molecular Excitons, Springer, New York, 2013.

- M. Kasha, H. R. Rawls, M. A. El-Bayoumi, Pure Appl. Chem. 1965, 11, 371.

- H. Eichhorn, D. Wöhrle, D. Pressner, Liq. Cryst. 1997, 22, 643.

- Tolbin A.Yu., Tomilova L.G., Zefirov N.S. Russ. Chem. Rev. 2008, 77, 435-449

- A.G. Martynov, Yu.G. Gorbunova, A.Yu. Tsivadze, Russian J. Inorg. Chem., 2014, 59, 1635.

- N. Kobayashi, H. Lam, W.A. Nevin, P. Janda, C.C. Leznoff, A.B.P. Lever, Inorg. Chem. 1990, 29, 3415.

- Y. Yamada, T. Maeno, K. Nawate and K. Tanaka, Chem. Commun., 2018, 54, 8226.

- S.G. Makarov, K.N. Maksimova, E.V. Baranov, G.K. Fukin, O. N. Suvorova, D. Wöhrle, G.A. Domrachev, Russ. Chem. Bull., 2006, 55, 1748.

- Y. Asano, M. Uchiyama, A. Fukasawa, T. Hatano, A. Muranaka and N. Kobayashi, J. Am. Chem. Soc., 2007, 129, 4516.

- Y. Asano, J. Sato, T. Furuyama, N. Kobayashi, Chem. Commun., 2012, 48, 4365

- L. Zhao, X. Ren, X. Yan, CCS Chem. 2021, 3, 678.

- J.E. Norton, J.-L. Bredas, J. Chem. Phys., 2008, 128, 034701.

- B.L. Wheeler, G. Nagasubramanian, A.J. Bard, L.A. Schechtman, D.R. Dininny, M.E. Kenney, J. Am. Chem. Soc. 1984, 106, 7404.

- G. De La Torre, A. Hausmann, M. Sekita, G. Bottari, T. Torres and D. M. Guldi, Chem. Soc. Rev., 2013, 42, 8049.

- T. Mirkovic, R. Van Grondelle, E.E. Ostroumov, J.M. Anna, G. Govindjee, G.D. Scholes, Chem. Rev. 2017, 117, 249.

- J. L. Bredas, D. A. Da Silva Filho, J. Cornil and J. P. Calbert, PNAS, 2002, 99, 5804

- S. Yanagisawa, I. Hamada, K. Yamauchi, T. Oguchi and T. Inaoka, Phys. Rev. B, 2014, 90, 245141.

- L. P. Doctor, F. Ziegs, B. Büchner, M. Naumann, A. Popov and M. Knupfer, J. Phys. Chem. C, 2021, 125, 12398.

- M. Kato, J. Onoe, Y. Matoba, K. Okamoto, S. Watanabe, J.-P. Bucher, M. Nakaya, J. Chem. Phys., 2020, 153, 144704.

- N.J. Hestand, F.C. Spano, Acc. Chem. Res., 2017, 50, 341.

- A.O. Gudovannyy, J.M. Schäfer, O. Gerdes, D. Hildebrandt, G. Mattersteig, M. Pfeiffer, F. Ortmann, Adv. Funct. Mater. 2025, 2421048

- Sergei, this is already Ref 8!   S. G. Makarov, G. Schnurpfeil, S. Y. Ketkov and D. Wöhrle, J. Porphyrins Phthalocyanines, 2020, 24, 515.

- Sergei this is already Ref 9!   S. G. Makarov, S. Y. Ketkov, D. Wöhrle and G. Schnurpfeil, Journal of Porphyrins and Phthalocyanines, 2021, 25, 236

- J.P. Heindel, K.M. Herman, E. Apra, S.S. Xantheas, J. Phys. Chem. Lett., 2021, 12, 7574

- H. Isago, Optical Spectra of Phthalocyanines and Related Compounds, Springer, Japan, 2015.

- R. D. Harcourt, G. D. Scholes, K. P. Ghiggino and S. Speiser, J. Chem. Phys., 1996, 105, 1897.

- D.L. Dexter J. Chem. Phys. 1953, 21, 836.

- T. Renger, F. Müh, Photosynth. Res., 2012, 111, 47.

- P.M. Kazmaier, R. Hoffmann, J. Am. Chem. Soc. 1994, 116, 9684-9691.

- H. Jiang, Y. Li, C. Kloc, J. Ye, Y. Long, D. Fichou, W. Hu, R. Ganguly ,P. Hu, Angew. Chem. Int. Ed. 2018, 57, 10112.

- J. Torras, C. Aleman, J. Casanovas, J. Phys. Chem. A, 2012, 116, 7571.

- J.-L. Bredas, Mater. Horiz., 2014, 1, 17.

- R.E. Larsen, J. Phys. Chem. C, 2016, 120, 9650.

- W.R. Scheidt, W. Dow, J. Am. Chem. Soc., 1977, 99, 1101.

- A. D. Becke, Phys. Rev. A, 1988, 38, 3098.

- C. Lee, W. Yang, R. G. Parr, Phys. Rev. B, 1988, 37, 785.

- H. Iikura, T. Tsuneda, T. Yanai, K. Hirao, J. Chem. Phys., 2001, 115, 3540.

- F. Weigend, R. Ahlrichs, Phys. Chem. Chem. Phys., 2005, 7, 3297.

- F. Weigend, Phys. Chem. Chem. Phys., 2006, 8, 1057.

- A.D. Becke, J. Chem. Phys., 1993, 98, 5648.

- J.P. Perdew, Y. Wang, Phys. Rev. B, 1992, 45, 13244.

- W.J. Hehre, R. Ditchfield, J.A. Pople, J. Chem. Phys., 1972, 56, 2257.

- P.C. Hariharan, J.A. Pople, Theor. Chem. Acc., 1973, 28, 213.

- V. A. Rassolov, J. A. Pople, M. A. Ratner, T. L. Windus, J. Chem. Phys., 1998, 109, 1223.

- A.A. Granovsky, Firefly version 8.2.0, www http://classic.chem.msu.su/gran/firefly/index.html

- M.W. Schmidt, K.K. Baldridge, J.A. Boatz, S.T. Elbert, M.S. Gordon, J.H. Jensen, S. Koseki, N. Matsunaga, K.A. Nguyen, S.J. Su, T.L. Windus, M. Dupuis, J. A. Montgomery, J. Comput. Chem., 1993, 14, 1347.

- F. Neese, Wiley Interdiscip. Rev.: Comput. Mol. Sci., 2025, 15, e70019.

- B.I. Dunlap, J. Chem. Phys., 1983, 78, 3140.

- F. Neese, F. Wennmohs, A. Hansen and U. Becker, Chem. Phys., 2009, 356, 98.

- C.M. Breneman, K.B. Wiberg, J. Comput. Chem., 1990, 11, 361.

- T. Lu and F. Chen, J. Comput. Chem., 2012, 33, 580.